**PPGI color coated galvanized steel plate in coil JIS standard SGCC grade**





Product Details

|  |  |
| --- | --- |
| Size | (0.13mm-5.0mm )\*(600mm-1500mm)\*coil |
| Steel Grade | JIS G3302 SGCC~SGC570,SGCH(FULL HARD-G550),SGHC~SGH540EN 10346-DX51D+Z,DX53D+Z, S250GD~S550GDASTM A653M CS-B, SS255~SS550 |
| Coil Weight | 3MT-14MT |
| Coil ID | 508mm/610mm |
| Chemical Treatment | Chromated(Cr 3+,6+,0+) |
| Surface | chromed / skinpass/ oiled/slightly oiled/ dry/ anti-fingerprint |
| Oil | Slight Oiled/Dry |
| Spangle | Regular/Zero/Big |
| Zinc Coating | Z40-Z300 |
| Capacity | 1,500,000MT/year |
| Mill Origin | HBIS-Tangsteel,Shandong Zhongguan, Changshu Everbright, WISCO |

Standard and Grade of HDG steel sheet/coil PPGI/PPGL

|  |  |  |  |
| --- | --- | --- | --- |
| NAME | PPGI | GALVANIZED | GALVALUME/ALUZINC |
|  STANDARD | EN10142JIS G3302GB/T-12754-2006 | ASTM A653JIS G3302SGCC/SGCHGB/T2518European Standard | ASTM A792JIS G3321JIS G3317 |
|  GRADE | CGCCCGCHCGCD1-CGCD3CGC340-CGC570GRADE | SS GRADE33-80SGCCSGCHSGCD1-SGCD3SGC340-SGC570SGCCDX51D | GRADE33-80SGLCCSGLCDSGLCDDSGLC400-SGLC570SZACCSZACHSZAC340R |
| MODEL NO | 0.16MM-1.5MM\*1250MM OR UNDER | (0.12-1.5)\*1250MM OR UNDER | 0.16MM-1.5MM\*1250MM OR UNDER |
|  TYPE | Steel coilSteel sheets/platesCorrugated steel sheets/plates | Steel coilSteel sheets/platesCorrugated steel sheets/plates | Steel coilSteel sheets/platesCorrugated steel sheets/plates |
| TECHNIQUE | Hot rolled-cold rolled-galvalume /galvanized-PPGI/PPGL | Hot rolled-cold rolled- galvanized | Hot rolled-cold rolled-galvalume /Aluzinc |
| SURFACETREATMENT | Mini/regular/big/zero spangle,Chromate treatment /chromate-free treatment /untreated unoile/oiled,TENSION LEVELLERT SKIN PASS anti-fingerprint/un-anti-fingerprint,Coating,color | Mini/regular/big/zero spangle,Chromate treatment /chromate-free treatment /untreated unoile/oiled,TENSION LEVELLERT SKIN PASS anti-fingerprint/un-anti-fingerprint,Coating |
| APPLICATION | Structural use ,roofing, commercial use, household appliance, industry, family |
| SPECIALAPPLICATION | Wear resistant steel, high- strength - steel plate |



|  |  |  |  |
| --- | --- | --- | --- |
| NAME | PPGI | GALVANIZED | GALVALUME/ALUZINC |
|  STANDARD | EN10142JIS G3302GB/T-12754-2006 | ASTM A653JIS G3302SGCC/SGCHGB/T2518European Standard | ASTM A792JIS G3321JIS G3317 |
|  GRADE | CGCCCGCHCGCD1-CGCD3CGC340-CGC570GRADE | SS GRADE33-80SGCCSGCHSGCD1-SGCD3SGC340-SGC570SGCCDX51D | GRADE33-80SGLCCSGLCDSGLCDDSGLC400-SGLC570SZACCSZACHSZAC340R |
| MODEL NO | 0.16MM-1.5MM\*1250MM OR UNDER | (0.12-1.5)\*1250MM OR UNDER | 0.16MM-1.5MM\*1250MM OR UNDER |
|  TYPE | Steel coilSteel sheets/platesCorrugated steel sheets/plates | Steel coilSteel sheets/platesCorrugated steel sheets/plates | Steel coilSteel sheets/platesCorrugated steel sheets/plates |
| TECHNIQUE | Hot rolled-cold rolled-galvalume /galvanized-PPGI/PPGL | Hot rolled-cold rolled- galvanized | Hot rolled-cold rolled-galvalume /Aluzinc |
| SURFACETREATMENT | Mini/regular/big/zero spangle,Chromate treatment /chromate-free treatment /untreated unoile/oiled,TENSION LEVELLERT SKIN PASS anti-fingerprint/un-anti-fingerprint,Coating,color | Mini/regular/big/zero spangle,Chromate treatment /chromate-free treatment /untreated unoile/oiled,TENSION LEVELLERT SKIN PASS anti-fingerprint/un-anti-fingerprint,Coating |
| APPLICATION | Structural use ,roofing, commercial use, household appliance, industry, family |
| SPECIALAPPLICATION | Wear resistant steel, high- strength - steel plate |



















